## Slide 1
LEO 1530 SEM Magnification Calibration Results, 3rd quarter (Dec-Feb)
Voltage/ Direction | Magnification 1000X | Magnification 10Kx | Magnification 50 Kx | Magnification 100Kx
@ 5 kV Horizontal Vertical | -2.0% - 2.65% | -2.15% -2.15% | -1.08% -2.16% | -2.59% -2.38%
@10 kV Horizontal Vertical | -2.65% -2.14% | -2.15% -1.94% | -2.16% -0.65% | -2.59% -0.73%