NIST Reference sample analyzed on the MRD. Peaks and relative intensities match against the reference.

## Measurement Conditions

Dataset Name	NIST_ReferenceA_05162021MRD

File name	C:\XRD Data\NIST_Reference\NIST_ReferenceA_05162021MRD.xrdml

Sample Identification	05162021MRD

Comment	Configuration=Mod FACTORY CONFIGURATION, Owner=User-1, Creation date=2/20/2008 4:58:19 PM

Goniometer=PW3050/65 (Theta/2Theta); Minimum step size 2Theta:0.0001; Minimum step size Omega:0.0001

Sample stage=MRD Cradle; Minimum step size Phi:0.01; Minimum step size Chi:0.01; Minimum step size X:0.01; Minimum step size Y:0.01; Minimum step size Z:0.001

Diffractometer system=XPERT-PRO

Measurement program=C:\PANalytical\Data Collector\Programs\NIST_ReferenceA.xrdmp, Identifier={043B9CEB-F149-4F1D-BA69-6A79672A9D6A}

Batch program=C:\PANalytical\Data Collector\Programs\nist batch 05162021.xrdmp, Identifier={7A7EB817-B51A-4B77-AD18-238CE0BEA8AC}

PHD Lower Level = 5.63 (keV), PHD Upper Level = 12.87 (keV)

Measurement Start Date/Time	5/16/2021 10:21:45 AM

Operator	user-1

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	20.0250

End Position [°2θ]	139.9750

Step Size [°2θ]	0.0500

Scan Step Time [s]	2.0000

Scan Type	Continuous

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.4354

Specimen Length [mm]	10.00

Receiving Slit Size [mm]	0.1000

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-Alpha1 [Å]	1.54060

Generator Settings	40 mA, 45 kV

Diffractometer Type	0000000013030338

Diffractometer Number	0

Goniometer Radius [mm]	320.00

Dist. Focus-Diverg. Slit [mm]	100.00

Incident Beam Monochromator	No

Spinning	No

## Main Graphics, Analyze View: (Bookmark 2)

## Peak List: (Bookmark 3)

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 25.2286 | 0.00 | 0.1416 | 3.52722 | 0.00 |
| 34.7623 | 0.00 | 0.1416 | 2.57861 | 0.00 |
| 37.3515 | 0.00 | 0.1416 | 2.40559 | 0.00 |
| 41.2719 | 0.00 | 0.1416 | 2.18569 | 0.00 |
| 42.9057 | 0.00 | 0.1416 | 2.10617 | 0.00 |
| 45.7071 | 0.00 | 0.1416 | 1.98338 | 0.00 |
| 52.0518 | 0.00 | 0.1416 | 1.75556 | 0.00 |
| 56.9857 | 0.00 | 0.1416 | 1.61472 | 0.00 |
| 59.1790 | 0.00 | 0.1416 | 1.56000 | 0.00 |
| 60.5616 | 0.00 | 0.1416 | 1.52765 | 0.00 |
| 60.7871 | 0.00 | 0.1416 | 1.52252 | 0.00 |
| 65.9219 | 0.00 | 0.1416 | 1.41582 | 0.00 |
| 67.5869 | 0.00 | 0.1416 | 1.38493 | 0.00 |
| 69.7983 | 0.00 | 0.1416 | 1.34636 | 0.00 |
| 73.6839 | 0.00 | 0.1416 | 1.28467 | 0.00 |
| 76.2653 | 0.00 | 0.1416 | 1.24748 | 0.00 |
| 76.6084 | 0.00 | 0.1416 | 1.24274 | 0.00 |
| 79.7374 | 0.00 | 0.1416 | 1.20166 | 0.00 |
| 79.9763 | 0.00 | 0.1416 | 1.19867 | 0.00 |
| 82.5000 | 0.00 | 0.1416 | 1.16828 | 0.00 |
| 82.5000 | 0.00 | 0.1416 | 1.16828 | 0.00 |
| 83.6076 | 0.00 | 0.1416 | 1.15560 | 0.00 |
| 84.3777 | 0.00 | 0.1416 | 1.14700 | 0.00 |
| 85.5804 | 0.00 | 0.1416 | 1.13393 | 0.00 |
| 85.7779 | 0.00 | 0.1416 | 1.13183 | 0.00 |
| 88.2763 | 0.00 | 0.1416 | 1.10613 | 0.00 |
| 90.0057 | 0.00 | 0.1416 | 1.08931 | 0.00 |
| 90.3778 | 0.00 | 0.1416 | 1.08579 | 0.00 |
| 93.9767 | 0.00 | 0.1416 | 1.05345 | 0.00 |
| 94.4103 | 0.00 | 0.1416 | 1.04975 | 0.00 |
| 97.4927 | 0.00 | 0.1416 | 1.02461 | 0.00 |
| 100.2190 | 0.00 | 0.1416 | 1.00395 | 0.00 |
| 101.9822 | 0.00 | 0.1416 | 0.99131 | 0.00 |
| 102.3632 | 0.00 | 0.1416 | 0.98866 | 0.00 |
| 103.6953 | 0.00 | 0.1416 | 0.97956 | 0.00 |
| 108.4845 | 0.00 | 0.1416 | 0.94923 | 0.00 |
| 108.9008 | 0.00 | 0.1416 | 0.94676 | 0.00 |
| 109.7541 | 0.00 | 0.1416 | 0.94178 | 0.00 |
| 109.9638 | 0.00 | 0.1416 | 0.94057 | 0.00 |
| 113.0076 | 0.00 | 0.1416 | 0.92371 | 0.00 |
| 114.9443 | 0.00 | 0.1416 | 0.91362 | 0.00 |
| 115.5986 | 0.00 | 0.1416 | 0.91032 | 0.00 |
| 116.6482 | 0.00 | 0.1416 | 0.90513 | 0.00 |
| 118.9839 | 0.00 | 0.1416 | 0.89408 | 0.00 |
| 120.7532 | 0.00 | 0.1416 | 0.88612 | 0.00 |
| 120.7532 | 0.00 | 0.1416 | 0.88612 | 0.00 |
| 123.3067 | 0.00 | 0.1416 | 0.87525 | 0.00 |
| 126.3515 | 0.00 | 0.1416 | 0.86318 | 0.00 |
| 128.5330 | 0.00 | 0.1416 | 0.85511 | 0.00 |
| 128.5330 | 0.00 | 0.1416 | 0.85511 | 0.00 |
| 129.7771 | 0.00 | 0.1416 | 0.85070 | 0.00 |
| 130.7034 | 0.00 | 0.1416 | 0.84752 | 0.00 |
| 131.2261 | 0.00 | 0.1416 | 0.84576 | 0.00 |
| 134.4177 | 0.00 | 0.1416 | 0.83554 | 0.00 |
| 134.4177 | 0.00 | 0.1416 | 0.83554 | 0.00 |
| 137.6804 | 0.00 | 0.1416 | 0.82599 | 0.00 |
| 138.8916 | 0.00 | 0.1416 | 0.82267 | 0.00 |
| 139.1927 | 0.00 | 0.1416 | 0.82186 | 0.00 |

## Pattern List: (Bookmark 4)

| Visible | Ref.Code | Score | Compound Name | Displ.[°2θ] | Scale Fac. | Chem. Formula |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-071-1683 | Unmatched Strong | Aluminum Oxide | 0.000 | 0.046 | Al2 O3 |